## Slide 1
Linear Spin Wave Calculations with SpinW part I
Notes: 1

## Slide 2
Overview
Linear Spin Wave Theory
  Magnetic Hamiltonian
  Holstein-Primakoff expansion
  Diagonalisation
  Incommensurate single-k structure
SpinW
  Hamiltonian parameters (exchange, anisotropy) input
  Magnetic structure input
  Plotting the model
  Structure refinement
  Dispersion calculation

## Slide 3
SpinW can solve the magnetic Hamiltonian:
It uses the convention that:
  Positive values of the exchange J means an antiferromagnetic interaction.
  Positive values of the single ion anisotropy A means an easy-plane anisotropy.
The Hamiltonian above usually leads to magnetic ordering below a critical temperature.
Spin waves are the collective excitations of this ordered state.
Hamiltonian
General bi-linear
interactions
Single-ion
anistropy
Applied magnetic
field (Zeeman)

## Slide 4
Spin waves arise from deviations of the ordered magnetic state.
We use the spin deviations as the basis states for calculating the magnetic Hamiltonian.
The Hamiltonian is then partly solved by a Fourier transform
  For a ferromagnet the FT diagonalises the Hamiltonian
  More generally another transformation is required to diagonalise H.
The eigenvalues of H(q) gives the magnon energies and the eigenvectors can be used to calculate the spin-spin correlation function and INS intensity.
Steps in a Spin Wave Calculation

## Slide 5
Express the spin operators as the ladder operators:
Map the raising / lowering operators to bosonic creation and annihilation operators taking only terms linear in
Holstein-Primakoff Transformation
vs
ground state is fully
saturated state.
nth magnon is nth
deviation from this
linear spin wave theory means ignoring the terms
in blue.

## Slide 6
Hamiltonian
We could now substitute the Holstein-Primakoff operators back into the Hamiltonian, but then the maths gets complicated because of the dependence of the operators on the magnetic structure (spin orientation).
Instead we define a set of 3x3 rotation matrices Ri which rotates all the spin to ferromagnetic alignment, e.g.:
Where Si’ are all ferromagnetic.
Remembering that:
If we define two sets of vectors ui formed from the first two columns of the matrix Ri and vi formed from the third column as:
Then we have:
Where the bar indicates complex conjugation.

## Slide 7
Hamiltonian
The Hamiltonian thus becomes:
The terms in curly braces can be expressed as a vector of the H-P operators (basis states), giving:
Where Hij is a 2n x 2n matrix whoes matrix elements can be determined by the braced expressions above and is given in the SpinW paper.
The expression above will contain terms which mix spins at i and j – a Fourier Transform will separate this, e.g. as in:
We now Fourier transform the Hamiltonian and diagonalise it for every q point.

## Slide 8
Incommensurate Structure
Remember that we introduced a rotation matrix which rotates every spin into the ferromagnetic state – actually SpinW introduces two such rotations.
The first applies to all spins within a crystalline unit cell and is used for the “incommensurate” (single-q) calculations.
The second then rotates the spins within a unit cell into the ferromagnetic state.
It turns out that for structures which can be described by a rotation from one unit cell to another, that the spin-spin correlation function (and hence INS intensity S(Q,ω)) has three branches:
  At Q
  At Q ± k , where k is the ordering wavevector / magnetic propagation vector
Expressions for the spin-spin correlation function can be found in the SpinW paper:
S. Toth and B. Lake, J. Phys.: Condens. Matter, 27 (2015) 166002

## Slide 9
Questions so far?

## Slide 10
SpinW is written as a Matlab class:
There are three main things you need to define for a calculation:
SpinW
There is extensive online help/documentation at spinw.org, including presentations and tutorials

## Slide 11
SpinW uses three coordinate systems:
  Lattice units (l.u.) – defines the atomic positions; set by the unit cell parameters (a,b,c,α,β,γ)
  Reciprocal lattice units (r.l.u.) – defines the momentum transfer Q and magnetic propagation k vectors.
  Cartesian coordinates – defined w.r.t. lattice coordinates by x||a, z⊥(a,b) and y⊥(x,z). Used for:
    J, A, g matrices (exchange, SIA, g-tensor)
    Magnetic field directions
    Magnetic moment (spin) directions
    Components of the spin-spin correlation function.
SpinW

## Slide 12
To start, you have to create a spinw object. You can:
  Start from scratch: >> swobj = m.spinw()
  Use a CIF or FST file: >> swobj = m.spinw('mycompound.cif')
Often it’s easier to start from scratch because usually you’re just interested in the magnetic atoms and can ignore everything else.
That just created a frustrated Cu square-lattice.
SpinW – Getting Started
swobj = m.spinw()
swobj.genlattice('lat_const', [3,3,5], 'angled', [90, 90, 90])
swobj.addatom('r', [0,0,0], 'S', 1/2, 'label', 'MCu2')
swobj.gencoupling('maxDistance', 5)
swobj.addmatrix('label', 'J1', 'value', 1)
swobj.addcoupling('mat', 'J1', 'bond', 1)
swobj.addmatrix('label', 'J2', 'value', 0.5)
swobj.addcoupling('mat', 'J2', 'bond', 2)
plot(swobj)

## Slide 13
To start, you have to create a spinw object. You can:
  Start from scratch: >> swobj = m.spinw()
  Use a CIF or FST file: >> swobj = m.spinw('mycompound.cif')
Often it’s easier to start from scratch because usually you’re just interested in the magnetic atoms and can ignore everything else.
That just created a frustrated Cu square-lattice.
SpinW – Getting Started
swobj = m.spinw()
swobj.genlattice('lat_const', [3,3,5], 'angled', [90, 90, 90])
swobj.addatom('r', [0,0,0], 'S', 1/2, 'label', 'MCu2')
swobj.gencoupling('maxDistance', 5)
swobj.addmatrix('label', 'J1', 'value', 1)
swobj.addcoupling('mat', 'J1', 'bond', 1)
swobj.addmatrix('label', 'J2', 'value', 0.5)
swobj.addcoupling('mat', 'J2', 'bond', 2)
plot(swobj)

## Slide 14
All exchange, SIA, g-tensors defined as 3x3 matrices.
The addmatrix method has the following shortcuts:
  A scalar input v means the matrix is the identity times v
  A vector input [Mx,My,Mz] defines an antisymmetric matrix:
So adding a DM interaction with a DM vector along [110] is:
SpinW
swobj.gencoupling('maxDistance', 5)
swobj.addmatrix('label', 'J1', 'value', 1);
swobj.addcoupling('mat', 'J1', 'bond', 1);
swobj.addmatrix('label', 'DM', 'value', [1,1,0]);
swobj.addcoupling('mat', 'DM', 'bond', 1);

## Slide 15
Single-ion anisotropy terms can usually be specified using the Matlab diag command – given a n-element vector it returns an n x n matrix with the diagonal elements being elements of that vector, e.g.
SpinW – Getting Started
swobj.addmatrix('label', 'K', 'value', m.diag([0, 0, -0.1]))
swobj.addaniso('K')
plot(swobj)

## Slide 16
Questions so far?

## Slide 17
day3_spinw1.ipynb

## Slide 18
The jth moment in the lth unit cell at t from the origin can be expressed as:
For a single-k structure, we omit the sum:
where Ψ is the complex basis vector and k is the propagation vector.
SpinW – Magnetic Structures
In SpinW, the magnetic structure is stored as a structure with fields:
Note that although SpinW uses these fields to store the magnetic structure, it can only truly handle incommensurate structures which can be represented by a rotation from one unit cell to the next.
mag_str.F | The complex basis vector in Cartesian units
mag_str.k | The propagation vector in reciprocal lattice units
mag_str.nExt | The magnetic supercell size in lattice units

## Slide 19
SpinW – Magnetic Structures
The supercell mode allows SpinW to describe arbitrary magnetic structures – at the cost of more intensive computation.
In this mode, every spin in every unit cell has to be specified.
E.g. 1D spin chain
mag_str.N_ext = [1 1 1];
mag_str.k = [1/2 0 0];
mag_str.F = [0;
1;
0];
mag_str.N_ext = [2 1 1];
mag_str.k = [0 0 0];
mag_str.F = [0 0;
1 -1;
0 0];
Single-k incommensurate mode
Supercell mode

## Slide 20
SpinW – Magnetic Structures
The supercell mode allows SpinW to describe arbitrary magnetic structures – at the cost of more intensive computation.
In this mode, every spin in every unit cell has to be specified.
E.g. triangular lattice
antiferromagnet
mag_str.N_ext = [1 1 1];
mag_str.k = [1/3 1/3 0];
mag_str.F = [1;
i;
0];
mag_str.N_ext = [3 3 1];
mag_str.k = [0 0 0];
mag_str.F = [1 -0.5 -0.5 -0.5 -0.5 1 -0.5 1 -0.5;
0 0.86 -0.86 0.86 -0.86 0 -0.86 0 0.86;
0 0 0 0 0 0 0 0 0];
Single-k mode
Supercell mode

## Slide 21
SpinW – Magnetic Structures
In SpinW, the magnetic structure is stored as a structure with fields:
You can directly set these fields, but it’s usually easier to use the genmagstr method. This has several modes:
  'helical' – extend a given structure by applying rotations between unit cells. Moments given either in the rotating frame notation as moments 'S' and a rotation axis 'n' or as complex vectors 'S'. Propagation vector 'k' determines the rotation angle between cells.
  'fourier' – similar to 'helical' but 'S' denotes the Fourier components – useful for sinusoidal amplitude modulated structures.
  'direct' – input the structure directly (every moment specified in 'S') – supercell structures usually specified by 'direct'.
  'random' – spins chosen at random. Used for simulated annealing determination of structures from exchange.
  'func' – generates a structure using a function (either user defined or there are built-in functions for planar and spherical single-k structures)
mag_str.F | The complex basis vector in Cartesian units
mag_str.k | The propagation vector in reciprocal lattice units
mag_str.nExt | The magnetic supercell size in lattice units

## Slide 22
Some examples:
SpinW – Magnetic Structures
tri = m.spinw()
tri.genlattice('lat_const', [4, 4, 6], 'angled', [90, 90, 120])
tri.addatom('r', [0, 0, 0], 'S', 2, 'label', 'MCr3', 'color', 'gold')
tri.genmagstr('mode', 'helical', 'S', [[1], [0], [0]],
'n', [0, 0, 1], 'k', [1/3, 1/3, 0])

## Slide 23
Some examples:
SpinW – Magnetic Structures
mmod = m.spinw()
mmod.genlattice('lat_const', [4, 4, 6], 'angled', [90, 90, 90])
mmod.addatom('r', [0.5, 0.5, 0.5], 'S', 2, 'label', 'MCr3', 'color', 'y')
mmod.genmagstr('mode', 'fourier', 'S', [[0], [1], [0]], 'k', [0.07, 0 0])

## Slide 24
Some examples:
SpinW – Magnetic Structures
sq = m.spinw()
sq.genlattice('lat_const', [4, 4, 6], 'angled', [90, 90, 90])
sq.addatom('r', [0.5, 0.5, 0.5], 'S', 2, 'label', 'MCr3', 'color', 'y');
sq.genmagstr('mode', 'direct',
'S', [[0, 0, 0, 0], [1, -1, -1, 1], [0, 0, 0, 0],
'nExt', [2, 2, 1])

## Slide 25
Some examples:
SpinW – Magnetic Structures
fct = m.spinw()
fct.genlattice('lat_const', [4, 4, 6], 'angled', [90, 90, 90])
fct.addatom('r', [0, 0, 0], 'S', 2, 'label', 'MCr3', 'color', 'gold')
fct.addatom('r', [0.5, 0.5, 0], 'S', 2, 'label', 'MCr3', 'color', 'k')
fct.genmagstr('mode', 'func', 'func', m.eval('@gm_planar'),
'x0', [0, np.pi/2, 1/2, 1/2, 1, 0, 0])

## Slide 26
Some examples:
SpinW – Magnetic Structures
fct = m.spinw()
fct.genlattice('lat_const', [4, 4, 6], 'angled', [90, 90, 90])
fct.addatom('r', [0.5, 0.5, 0], 'S', 2, 'label', 'MCr3', 'color', 'gold')
fct.genmagstr('mode', 'random', 'nExt', [2, 2, 1])

## Slide 27
Often the initial magnetic structure you input doesn’t quite agree with the exchange parameters you put in – this will result in a “non-Hermitian Hamiltonian” error.
SpinW contains several functions to optimise the magnetic structure to minimise the classical magnetic ground state energy:
  optmagsteep – optimise a magnetic structure succesively rotating each moment to the Weiss field direction.
    Fast, but will not change the super-cell size or the propagation vector.
  optmagk – optimises the propagation vector by finding the k which minimises the eigenvalues of the (Fourier transformed) Hamiltonian
  optmagstr – nonlinear search for optimal structure (using fminsearch) but needs a function to set the structure.
  anneal – performs simulated annealing using the Metropolis algorithm, can be used to calculate thermodynamic properties.
Magnetic Structure Optimisation

## Slide 28
Questions so far?

## Slide 29
Once the Hamiltonian (exchange, SIA, etc) and magnetic structure is set, SpinW can calculate the spin wave dispersion and the INS spectrum:
Q can be a 3xN array of Q points to calculate at
Or a Matlab cell-array (Python tuple) with Q points to plot along, and the number of points per segment e.g.
Dispersion calculations
spec = swobj.spinwave(Q, 'parameter', 'value', ...)
spec = swobj.spinwave(([0,0,0], [1,1,1], [1,0,0] 200));
m.sw_plotspec(spec)

## Slide 30
Use sw_plotspec to plot the spectrum returned by spinwave.
Need to use sw_egrid to bin the dispersion and calculate the INS intensity:
Dispersion calculations
spec = swobj.spinwave(([0,0,0], [1,1,1], [1,0,0] 200))
spec = m.sw_egrid(spec)
m.sw_plotspec(spec, 'dE', 0.1)

## Slide 31
The parameters which spinwave accepts include:
  'formfact' – (default: false) whether to include the magnetic form factor in the calculation of the spin wave intensity.
  'hermit' – (default: true) whether to use a Hermitian only algorithm to diagonalise the Hamiltonian. In cases where the magnetic structure does not match the Hamiltonian parameters, you can get a non-Hermitian Hamiltonian and if 'hermit' is true then spinwave will return an error. Set to false if you want to force the calculation – but plot the result and check that the maximum energy of the imaginary modes is low.
  'optmem' – (default: 0 [auto]) how many chunks to split the input Q vectors into – SpinW runs fastest when it can load everything into memory to run through all the Q-vectors at once; but sometimes this is not possible due memory constraints; by default it checks how much free memory there is and picks a suitable number of chunks. But you can also override it if you are running out of memory or SpinW underestimates the amount of free memory.
  Other parameters: see online help
Dispersion calculations

## Slide 32
Use powspec instead of spinwave to calculate a powder averaged spectrum.
Powder average
swobj = m.sw_model('triAF', 1)
modQ = np.linspace(0,3,100)
spec = swobj.powspec(modQ, 'nRand', 10000, 'Evect', np.linspace(0,4,200))
m.sw_plotspec(spec)

## Slide 33
Questions so far?

## Slide 34
Linear spin wave theory
  Strictly only valid for large S
  Requires an ordered magnetic state
SpinW
  Uses a rotating frame description which can calculate certain single-k magnetic structure dispersion efficiently
  Need to define the Hamiltonian and magnetic structure before can calculate dispersion
  Can optimise the input magnetic structure to better agree with the Hamiltonian.
  Lots of examples / tutorials on spinw.org
Summary